| Publicity Print Publicity Print is a woodfree coated paper for productions where excellent printability in combination with high bulk is needed. This product is an excellent choice for high quality printing. The matt surface gives very good contrast and the bulk superior runnability. Publicity Print is available in various sizes in grammages from 90 to 250 g/m². Publicity Print has high stiffness and is especially prepared also for post-print production processes. |  | Ideal for: Impact Advertising Direct Mail Publicity Campaigns Posters Advertising inserts and cards Target Advertising Personalized Product Campaigns Product description Wood-free coated paper Finish matt Printing method offset Producer Grycksbo Mill |
| --- | --- | --- |

Technical specifications -  Publicity Print

| Grammage g/m2 | ISO 536 DIN 53104 | 90 | 100 | 115 | 130 | 150 | 170 | 200 | 230 | 250 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Bulk cm3/g | ISO 536:1995 | 0.91 | 0.92 | 0.93 | 0.96 | 0.98 | 0.98 | 1.04 | 1.04 | 1.04 |  |
| Whiteness CIE with D65/10% | ISO 11475 | 119 | 119 | 119 | 119 | 119 | 119 | 119 | 119 | 119 |  |
| Brightness with D65/10% | mod.ISO 2470 Modified | 97 | 97 | 97 | 97 | 97 | 97 | 97 | 97 | 97 |  |
| Opacity with D65/10 % | mod.ISO 2471 Modified | 92 | 94.5 | 96 | 97 | 98 | >98 | 99.1 | 99.5 | >99 |  |
| Gloss TAPPI 75 % | ISO/DIS 8245-1 T480 om-92 | 27 | 27 | 27 | 27 | 27 | 27 | 27 | 27 | 27 |  |
| Surface Roughness PPS 1.0 µm | DIN ISO 8791-4 | 1.8 | 1.8 | 1.8 | 1.8 | 1.8 | 1.8 | 2.2 | 2.2 | 2.2 |  |

| Reel specifications max. width cm min. width cm max. diameter cm min. diameter cm | Core mm 70 / 76 / 150 Wrapping | Environment Production/Certificates |
| --- | --- | --- |